| Surname |  | Group No |  | Personal Tutor: |
| --- | --- | --- | --- | --- |
| First Name |  | Discipline |  |  |

UNIVERSITY OF BIRMINGHAM

School of Engineering

Experiment AM1.6 - Mechanical Testing (Tensile)

Safety

- Make sure you know where the nearest fire exits are and what the evacuation procedure is.

- Make sure you know where the nearest first aiders are located and what their phone numbers are.

- Do not operate the machinery unless you have been instructed to do so by the supervisor.

- Ensure you are completely familiar with the controls before operating any equipment.

The final two points are critical for this laboratory: the test apparatus can cause serious harm if misused!

Learning outcomes

By the end of this experiment you should hopefully:

- understand how standard materials deform under load and their fracture;

- be able to calculate the elastic modulus of materials from raw data.

Description

The present laboratory examines the behaviour of two materials (carbon steel and aluminium), you are required to determine the:

- Young's modulus (see equations 1 -3);

- Yield stress;

- Ultimate tensile stress;

- Percentage elongation at fracture;

- Percentage reduction in cross-sectional area at fracture;

- Fracture stress.

E=σε		(1)

σ=FA 		(2) 		and 		ε=∆LL			(3)

where:

E is the Young’s modulus of a material; σ is the stress induced in the material; ɛ is the strain experienced by the material; F is the force applied to the test specimen; A is the cross-sectional area of the test specimen; ΔL is the extension of the test specimen, and L is its original length.

Procedure

The test pieces have been manufactured to BS18:Part 1, 1970. Two specimens will be tested: 0.1% carbon steel and aluminium (aluminium alloy 2011-T3); Figure 1. Each specimen should be measured in terms of length and diameter, with repeat measures taken along the test section to estimate the mean values (± standard deviation). Use Vernier callipers for measurements.

Insert the specimen into the MTS test machine. This machine is an industry standard test facility and calibrated to comply with ISO test standards. You will be told how to operate it by the demonstrator (Standard Operating Procedures are available on CANVAS). Briefly, specimens are to be placed in the gripping device, which is to be attached to the MTS actuator/cross-head and base. The protective screen should be in place, facing observers, to prevent any fragments from causing injury if ejected during failure of the test specimens. Note, when the actuator is ‘on’, no user or observer should touch (or be near) the actuator and/or other moving parts. The actuator should always be ‘off’ when specimens are being placed/removed and/or grips attached.

Figure 1. Test Specimens. Top: Aluminium, bottom: Carbon Steel.

Take note of the rate of loading used, and whether this is under load or displacement control. Observe the computer screen where the load vs. extension graph is generated automatically. Raw data will be provided on CANVAS following the session; however, note down at least 10 sets of force-displacement data (Table 1 for Carbon Steel; Table 2 for Aluminium), to enable you to plot the figures suggested in this report (Figure 2 and 3). Observe the test specimen for its elongation and fracture point during the test.

Following the test, take the test specimen and assess its failure (noting how fracture has occurred and the specimen shape following fracture). If possible, estimate its final diameter to enable the true stress at fracture to be estimated. Use force-displacement data to estimate the true strain.

Use the force-displacement data, from Table 1 and 2, to plot stress-strain graphs (Figure 2 and 3). Calculate a Young’s modulus for each test specimen, and aim to determine the Yield stress, ultimate tensile stress, percentage elongation at fracture, percentage reduction in cross-sectional area at fracture, and fracture stress. How do carbon steel and aluminium compare in terms of their material properties? How do their Young’s moduli, within their elastic limit, compare to values in literature?

Experiment AM1.6 - Completed Data Tables

Table 1: Force-elongation data for Carbon Steel

| Time (s) | Disp (mm) | Force (kN) | Stress (MPa) | Strain (%) | True Stress (MPa) | True Strain (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.1 | 0.0013 | 2.907 | 148.1 | 0.003 | 148.1 | 0.003 |
| 4.4 | 0.085 | 9.60 | 488.9 | 0.17 | 489.7 | 0.17 |
| 8.7 | 0.298 | 13.22 | 673.3 | 0.60 | 677.3 | 0.59 |
| 13 | 0.683 | 13.28 | 676.3 | 1.37 | 685.6 | 1.36 |
| 17.3 | 1.087 | 13.08 | 666.2 | 2.17 | 680.6 | 2.15 |
| 21.6 | 1.49 | 13.22 | 673.3 | 2.98 | 693.4 | 2.94 |
| 25.9 | 1.90 | 13.29 | 676.9 | 3.80 | 702.6 | 3.73 |
| 30.2 | 2.33 | 12.97 | 660.6 | 4.66 | 691.3 | 4.55 |
| 34.5 | 2.80 | 12.12 | 617.3 | 5.60 | 651.8 | 5.45 |
| 38.9 | 3.28 | 11.04 | 562.3 | 6.56 | 599.2 | 6.35 |

Table 2: Force-elongation data for Aluminium

| Time (s) | Disp (mm) | Force (kN) | Stress (MPa) | Strain (%) | True Stress (MPa) | True Strain (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.1 | 0.0023 | 2.766 | 140.9 | 0.005 | 140.9 | 0.005 |
| 5.5 | 0.248 | 6.22 | 316.8 | 0.50 | 318.4 | 0.50 |
| 10.9 | 0.673 | 6.93 | 352.9 | 1.35 | 357.7 | 1.34 |
| 16.3 | 1.109 | 7.414 | 377.6 | 2.22 | 386.0 | 2.19 |
| 21.7 | 1.557 | 7.74 | 394.2 | 3.11 | 406.5 | 3.07 |
| 27.1 | 2.017 | 7.96 | 405.4 | 4.03 | 421.7 | 3.95 |
| 32.5 | 2.48 | 8.08 | 411.6 | 4.96 | 432.0 | 4.84 |
| 37.9 | 2.97 | 8.14 | 414.6 | 5.94 | 439.2 | 5.77 |
| 43.3 | 3.46 | 8.14 | 414.6 | 6.92 | 443.3 | 6.69 |
| 48.7 | 3.98 | 7.74 | 394.2 | 7.96 | 425.6 | 7.66 |

Comments on results obtained

1. Comparison of Material Properties

- Young's Modulus ($E$):

  - Carbon Steel: Calculated from the initial slope (Force change ~6.7kN, Disp change ~0.084mm), the modulus is approximately 210 GPa. This matches standard literature values for steel perfectly.

  - Aluminium: The initial data points suggest the material yielded early (at approx 300 MPa). Standard 2011-T3 aluminium has a modulus of ~70 GPa. The lower apparent stiffness in the data may be due to machine compliance or an offset in the displacement gauge.

- Yield & UTS:

  - Carbon Steel: Shows a very high Ultimate Tensile Strength (UTS) of ~677 MPa. It exhibits clear necking behavior, as the stress drops significantly (from 677 to 562 MPa) before failure.

  - Aluminium: Shows a UTS of ~415 MPa. This aligns well with 2011-T3 alloy (typical UTS ~380-400 MPa). The drop in stress after UTS is less pronounced than in steel, indicating slightly different necking behavior.

2. Ductility and Fracture

- Elongation: The Aluminium specimen reached a higher strain (approx 8%) compared to the Carbon Steel (approx 6.5%) before the data ends. However, Steel is typically more ductile; the lower strain here might indicate the steel specimen failed earlier or was a high-strength brittle grade.

- Fracture Appearance:

  - Carbon Steel: Likely exhibited a "cup and cone" fracture surface, characteristic of ductile failure where microvoids coalesce.

  - Aluminium: Likely exhibited a shear fracture (45-degree angle) or a flatter surface, typical of semi-ductile aluminium alloys.

3. Comparison with Literature

- Steel: The experimental UTS (677 MPa) and Modulus (210 GPa) are consistent with medium-high carbon steel or cold-drawn steel.

- Aluminium: The experimental UTS (415 MPa) is consistent with high-strength aerospace/automotive alloys like 2011-T3. The Yield stress appears to be around 300-320 MPa, which also matches literature values for T3 temper (~295 MPa).

Graph